Anti-float Dispersing Agent

RD-904S

Features and advantages:

1. The dispersion and wetting effect of the pigment are excellent, and the color has good infiltration miscibility due to organosilicon.The presence of the ingredients has the effect of preventing the control of multi-colored flaring, flocculation and stripes.

2. Improve the wettability of the pigment and maintain its stability to prevent floating color, blooming and precipitation.

3. It can increase the gloss of the coating surface, reduce viscosity, prevent shrinkage and reduce orange peel phenomenon.

Product parameter:

| Appearance | Colorless to yellowish transparent liquid |
| --- | --- |
| Active ingredient | 30% |
| Constituent | Polyester modified silicone copolymer |

Recommended dosage:

| Entirety | 0.1–0.5% |
| --- | --- |
| Inorganic pigments | 3-10% |
| Organic pigments | 10-30% |

Usage:

In order to obtain full effect, please test the appropriate amount before use, please add before grinding.

Packing:

25KG non-recycled blue plastic drum. The product is not completely used, need to tighten the lid after use.

Storage:

Keep away from fire and light source and keep away from light.